Title: ПРАВИЛА ОФОРМЛЕНИЯ ТЕЗИСОВ КОНФЕРЕНЦИИ ВНКСФ-7
Author: Sergey Trapeznikov
Last saved by: Константин
Company: Saint-Petersburg State University

Специализация: 010700/03 Физика конденсированного состояния вещества
Программа: 24 Физика рентгеновских процессов в твёрдых телах
Руководитель программы: проф. А.С. Шулаков
Кафедра электроники твёрдого тела
Научный руководитель: проф. А.С. Виноградов
Рецензент: проф. А.А. Павлычев

Оксидирование монослоя гексагонального нитрида бора на Ir(111), контролируемое методами рентгеновской спектроскопии
Симонов Константин Алексеевич

В работе выполнено исследование влияния адсорбции атомарного кислорода на структурные и электронные свойства гексагонального нитрида бора (h-BN), выращенного на монокристаллической поверхности Ir(111). Процесс последовательного оксидирования контролировался поверхностно-чувствительными методами рентгеновской спектроскопии. 
Показано, что при комнатной температуре взаимодействие с атомарным кислородом в условиях сверхвысокого вакуума происходит путём замещения атомов азота в решётке h-BN атомами кислорода. Встраивание кислорода приводит к появлению четырёх типов химически неэквивалентных  позиций для атомов бора в исходных (BN_3) и кислород-замещённых (BN_3-xO_x, x = 1, 2, 3) структурных группах (квазимолекулах). Установлено, что именно это является причиной появления дополнительных π*-резонансов (a_1 - a_3) в ближней тонкой структуре BK-спектра поглощения окисленного h-BN. На основе анализа динамики процесса окисления установлен последовательный характер оксидирования монослоя h-BN: (i) при малых величинах экспозиции образуются преимущественно группы BN_2O; (ii) при увеличении времени оксидирования кислородосодержащие группы BN_2O становятся наиболее восприимчивы к встраиванию кислорода, что приводит к появлению структурных групп BNO_2 и BO_3. При этом замещение атомов азота в решётке h-BN сопровождается локальной деформацией монослоя.  Прогрев насыщенного кислородом образца вплоть до 600 °С приводит к образованию структуры подобной B_2O_3.
Отмечается, что механизмы окисления монослоёв h-BN и графита, выращенных на одной и той же подложке Ir(111), кардинально отличаются друг от друга. В случае графена, оксидирование происходит главным образом путём образования эпокси-групп, а прогрев образца приводит к десорбции кислорода (J. Phys. Chem. C. V. 115, 2011. P. 9568-9577).

Список публикаций

1. К.А. Симонов, M.М. Бржезинская, A.C. Виноградов, А.Б. Преображенский, А.В. Генералов, А.Ю.  Клюшин. Сравнительное исследование электронной структуры NiPc и CoPc методами рентгеновского поглощения и фотоэмиссии//Teзисы докладов VII национальной конференции РСНЭ – НБИК 2009, Москва, 16-21.11.2009. С. 236.

2. K.A. Simonov, A.S. Vinogradov, M.M. Brzhezinskaya, A.B.  Preobrajenski, A.V. Generalov, A.Yu. Klyushin. Comparative NEXAFS and resonant photoemission study of nickel and cobalt phthalocyanines//Conference Abstracts, International Student Conference “Science and Progress”, Saint-Petersburg-Peterhof, 15-19.11.2010. P. 103.

3. A.Yu. Klyushin, A.S. Vinogradov, A.V. Generalov, K.A. Simonov. Effects of chemical bonding on the resonant F KVV Auger electron emission from fluorinated multi-walled carbon nanotubes and polytetrafluoroethylene//Conference Abstracts, International Student Conference “Science and Progress”, Saint-Petersburg-Peterhof, 15-19.11.2010. P. 88.

4. T.V. Profe, A.S. Vinogradov, M.M. Brzhezinskaya, A.V. Generalov, A.Yu. Klyushin, K. A. Simonov. Comparative analysis of X-ray absorption spectra of ligand atoms in cyanide complexes of transition-metal atoms//Conference Abstracts, International Student Conference “Science and Progress”, Saint-Petersburg-Peterhof, 15-19.11.2010. P. 99.

5. K.A. Simonov, A.S. Vinogradov, M.M. Brzhezinskaya, A.B. Preobrajenski, A.V. Generalov, A.Yu. Klyushin. Comparative NEXAFS and resonant photoemission study of nickel and cobalt phthalocyanines//Conference Proceedings, International Student Conference “Science and Progress”, Saint-Petersburg-Peterhof, 15-19.11.2010. P.140.

6. A.Yu. Klyushin, A.S. Vinogradov, A.V. Generalov, K.A. Simonov. Effects of chemical bonding on the resonant F KVV Auger electron emission from fluorinated multi-walled carbon nanotubes and polytetrafluoroethylene//Conference Proceedings, International Student Conference “Science and Progress”, Saint-Petersburg-Peterhof, 15-19.11.2010. P.110.

7. T.V. Profe, A.S. Vinogradov, M.M. Brzhezinskaya, A.V. Generalov, A.Yu. Klyushin, K. A. Simonov. Comparative analysis of X-ray absorption spectra of ligand atoms in cyanide complexes of transition-metal atoms//Conference Proceedings, International Student Conference “Science and Progress”, Saint-Petersburg-Peterhof, 15-19.11.2010. P.130.

8. K.A. Simonov, N.A. Vinogradov, M.L. Ng, A.S. Vinogradov, N. Mårtensson, A. Preobrajenski. Oxidation of h-BN monolayer on Ir(111) studied by core-level spectroscopies//MAX-lab Activity Report 2010, MAX-lab, Lund, 2010. P. 428-429.

9. M.L. Ng, N. Vinogradov, K. Simonov, N. Mårtensson, A.B. Preobrajenski. Adsorbed graphene as a non-volatile platform for chemical reactions//MAX-lab Activity Report 2010, MAX-lab, Lund, 2010. P. 418-419.

10. А.С. Виноградов, М.М. Бржезинская, А.Б. Преображенский, Н.А. Виноградов, А.В. Генералов, А.Ю. Клюшин, К.А. Симонов. Характеризация атомной и электронной структуры углеродных материалов и наноструктур методами ультрамягкой рентгеновской спектроскопии//Сборник материалов Российско-Украинского семинара "Композиционные системы полимер-наноуглерод и различные физико-химические подходы к их исследованию", Санкт-Петербург, 25-27.05.2011, С. 23-24. (ISBN 978-5-905283-10-9).

11. N. Vinogradov, M.L. Ng, K. Simonov, N. Mårtensson, A.B. Preobrajenski. Reversible chemical reactions on adsorbed graphene//Book of Abstracts, Joint International Conference conference “Advanced Carbon Nanostructures”, ACN 2011, Saint-Petersburg 04.07-08.07.2011. P. 108.

12. A.Yu. Klyushin, А.S. Vinogradov, A.V. Generalov, K.A. Simonov. Chemical bonding effect on the resonant F KVV Auger emission from polytetrafluoroethylene//Book of Abstracts, Joint International Conference conference “Advanced Carbon Nanostructures”, ACN 2011, Saint-Petersburg 04.07-08.07.2011. P. 218.

13. Simonov K.A., Vinogradov A.S. , Brzhezinskaya M.M., Preobrajenski A.B., Generalov A.V. , Klyushin A.Yu. Features of electronic structure of nickel and cobalt phthalocyanines studied by core-level spectroscopies//Book of Abstracts, 11^th International Conference on Atomically Controlled Surfaces, Interfaces and Nanostructures, ASCIN 2011, Saint-Petersburg. 03.10-07.10.2011. P. 281.

14. K.A. Simonov, A.S. Vinogradov, M.M. Brzhezinskaya, A.B. Preobrajenski, A.V. Generalov, A.Yu. Klyushin. Features of metal atom 2p excitations and electronic structure of 3d-metal phthalocyanines studied by x-ray absorption and resonant photoemission//Appl. Surf. Sci., submitted (2012).

15. K.A. Simonov, N.A. Vinogradov, M.L. Ng, A.S. Vinogradov, N. Mårtensson, A.B. Preobrajenski. Controllable oxidation of h-BN monolayer on Ir(111) studied by core-level spectroscopies//Surf. Sci. V. 606, 2012. P. 564-570.

16. N.A. Vinogradov, K.A. Simonov, A.V. Generalov, A.S. Vinogradov, D.V. Vyalikh, C. Laubschat, N. Mårtensson, A.B. Preobrajenski. Controllable p-doping of graphene on Ir(111) by chlorination with FeCl_3//J. Phys.: Condens. Matter, submitted (2012).

17. N.A. Vinogradov, A.A. Zakharov, V. Kocevski, J. Rusz, K.A. Simonov, O. Eriksson, A. Mikkelsen, E. Lundgren, A.S. Vinogradov, N. Mårtensson, A.B. Preobrajenski. Non-equilibrium growth and structure of graphene on Fe(110)//Langmuir, submitted (2012).